## Slide 1: Chapter 6 Attributes of Prognostics Methods

## Slide 2: 1. Introduction

## Slide 3: Chapter Goal
Study on attributes of 5 prognostics algorithms
To provide guidelines so that the readers can choose an appropriate algorithm for their field of application
We will use simple and complex crack growth problems
advantages and disadvantages are discussed based on the logic of each algorithm
different prognostics algorithms have different characteristics
  Total form: use an explicit form of degradation as a function of model parameters, loading/usage condition and time/cycle
  Rate form: use a differential equation form of degradation model, where degradation level can be obtained by integrating the differential equation

## Slide 4: Model-Form Error
Models are developed under assumptions and simplifications
  Paris model: an infinite flat panel under mode I fatigue loading condition
Many model parameters are not intrinsic
  they depend on boundary conditions and loading conditions
  Parameters from lab tests may be different from that of field conditions
it is important how physics-based prognostics algorithms can correct or compensate for the model-form error

## Slide 5: Physics-based Methods
important to understand how different algorithms identify parameters
  especially uncertainty in model parameters and correlation between them
  Some algorithms represent this uncertainty in the form of samples
  Some assume Gaussian distribution with estimated variance
the prior knowledge on model parameters plays an important role in the performance of prognostics algorithm
  Bayesian-based algorithms have a systematic way of considering the prior knowledge
  regression-based algorithms do not have a feasible way of considering it

## Slide 6: Data-driven Methods
Looks more attractive as they don’t need physical model
  Especially for complex systems
But data-driven approaches also employ a mathematical model to represent the degradation behavior
  the mathematical model does not have any physical meaning
is the mathematical model good enough to represent the behavior of degradation?
  Complex model can represent complex degradation behavior
  Complex model has many parameters, which need to be identified with data
  Difficult to fit, over-fitting, under-fitting problems
  Normally (# of training data) > (2 ~ 3)*(# of unknown coefficients)
data-driven approaches move the decision of selecting model form to users

## Slide 7: 2. Problem Definition

## Slide 8: Paris Model for Fatigue Crack Growth
the rate of crack growth under constant amplitude cyclic mode I loading of an infinite plate
  Ex) a fatigue crack growth in fuselage panel of airplanes due to repeated pressurizations
Incremental form:
: half crack size
and : model parameters
: number of loading cycles
: range of stress intensity factor

## Slide 9: Paris Model for Fatigue Crack Growth cont.
Material parameters
  : slope in log-log graph of crack growth rate and stress intensity factor
  : y-intercept at
  These parameters are extrinsic properties: unit-dependent and loading-dependent
Total form
  Rate form (differential equation) needs to be integrated with initial crack size (also need to be included as a model parameter)
  the first term in the bracket is negative, while the second term is positive
  Large can make the term negative  the crack will grow faster as increases  crack goes infinity and becomes complex

## Slide 10: Paris Model for Fatigue Crack Growth cont.
Critical crack size
  Crack grows and becomes unstable
  When the stress intensity factor reaches the fracture toughness
  Critical crack size for mode 1 loading
Model parameter identification
  using measured crack size data at different loading cycles
  test results show some level of variability (noise)  identified model parameters may show a statistical distribution
  Model-form error: the effect of finite plate size and the curvature of the plate is ignored
Maintenance is required before

## Slide 11: Huang’s Model for Fatigue Crack Growth
Paris model: constant amplitude loading
Huang’s model: variable amplitude loading
  equivalent stress intensity factor and a modified Wheeler model
  depends on the stress ratio and the plastic zone size ahead of the crack tip
  can describe the phenomena of retardation and arrest due to overload, and the acceleration due to a state of underload following an overload
  When , (no crack shrink)
: threshold of stress intensity factor range

## Slide 12: Huang’s Model for Fatigue Crack Growth cont.
includes crack tip plasticity and crack closure after overloading
  : geometric factor
  :scaling factor for the loading ratio
  : correction factor for the loading sequence interaction
: Load ratio
: shaping exponents
: plastic zone size
: increment of the plastic zone size
: shaping exponent
: plastic zone size factor
: maximum stress intensity factor
: tensile yield strength
Subscript OL: overload

## Slide 13: Huang’s Model for Fatigue Crack Growth cont.
No total form model
  forward Euler integration method to calculate the crack size at a given cycle
  Accuracy depends on integration time interval
Matlab code [Huang]
  assumed that the plate has a 4mm-thickness and 150mm-width
  a geometry factor for finite plate is employed (lines 30-31)
  The shaping exponent is not considered since
  uncertainties in loading, thickness and width of plate are ignored
  Model parameters:

## Slide 14: Matlab Code Huang
%=== PROBLEM DEFINITION (Loading and Model Parameters) ======
dN=1; % transition cycle interval
dtMeasu=1000; % measurement cycle interval
dSmin=5; % min. load
sNomin=65; % nominal load
sOverl=[125 100 100 125 125]; % overload
cNomin=[5 5 5 5 45]; % num. of cycle in a block: nominal load
cOverl=[45 45 95 95 5]; % num. of cycle in a block: overload
cBlock=[5000 10000 15000 20000 25000];% cycles for each block
a0=0.01; % true model param including initi crack, a0
m=3.1; C=log(5.5e-11); dKth=5.2; beta=0.2; n=2.8; sY=580;
thick=4e-3; width=150e-3/2; % geometry dimension
%============================================================
cycle=[0:dtMeasu:cBlock(end)]';
% % % LOAD RATIO, R
nb=length(cBlock);
cInter(1)=cBlock(1);
if nb>1; for i=2:nb; cInter(i)=cBlock(i)-cBlock(i-1); end;end

## Slide 15: Matlab Code Huang cont.
dSmax=[];
for i=1:nb;
B=[sNomin*ones(cNomin(i),1); sOverl(i)*ones(cOverl(i),1)];
dSmax(length(dSmax)+1:cBlock(i),1)= ...
repmat(B,cInter(i)/(cNomin(i)+cOverl(i)),1);
end;
dSmax=dSmax(1:dN:end); R=dSmin./dSmax;
% % % HUANG's MODEL
aCurre(1)=a0; akOL(1)=a0; rOL(1)=0;
for k=1:max(cycle)/dN;
ak=aCurre(k);
Y=(1-ak./(2*width)+0.326.*(ak./width).^2)...%geometry factor
./sqrt(1-ak./width); loca=ak./width>1; Y(loca)=0;
Kmax=Y.*dSmax(k).*sqrt(pi*ak); %SIF from Eq. 6.5
Kmin=Y.*dSmin.*sqrt(pi*ak);
% Scaling factor, Mr (Eq. 6.6)
Mr=(1-R(k)).^(-beta);

## Slide 16: Matlab Code Huang cont.
% Correction factor, Mp (Eqs. 6.7 and 6.8)
alpha=0.35-0.29./(1+(1.08.*Kmax.^2./(thick.*sY.^2)).^2.15);
ry=alpha.*(Kmax./sY).^2;
if R(k)~=dSmin/sNomin;
loca=ry>rOL; rOL(loca)=ry(loca); akOL(loca)=ak(loca);
end
Mp=(ry./(akOL+rOL-ak)).^n; loca=ak+ry>=akOL+rOL; Mp(loca)=1;
% Calculate crack size
dKeq=Mr.*Mp.*(Kmax-Kmin); % Eq. 6.5
rate=exp(C).*(dKeq.^m - dKth.^m); % Eq. 6.4
loca=dKeq<=dKth; rate(loca)=0;
aCurre(k+1)=aCurre(k)+rate.*dN;
end;
crackHuang=aCurre(1:dtMeasu/dN:max(cycle)/dN+1);
% % % DATA PLOT
plot(cycle,crackHuang);

## Slide 17: Health Monitoring Data and Loading Conditions
Synthetic data
  The true values of model parameters and loading conditions are assumed
  With true parameters and loading conditions, the physical model at different times is used to generate true degradation data
  Random noise and deterministic bias are added to the true degradation data
  Synthetic data make it possible to compare the identified parameters with the true parameters
  possible to evaluate the accuracy of prediction remaining useful life
  possible to control the level of noise and bias such that their effect can be studied
True parameters
  Paris model parameters:
  Huang’s mode parameters:

## Slide 18: Health Monitoring Data and Loading Conditions
Data for Paris model
  10 sets of true data by gradually increasing stress from 65 MPa to 83 MPa
  Each set has 26 data until 2500 cycles (every 100 cycles)
  Critical crack size

## Slide 19: Health Monitoring Data and Loading Conditions
Data for Huang’s model
  10 data sets with crack retardation and acceleration due to complex loadings
  a loading block: fixed 5 MPa minimum load, two maximum loads (nominal load and overload)
  Table shows 5 loading blocks scenario (5,000 cycles for each block)

## Slide 20: Health Monitoring Data and Loading Conditions
Data for Huang’s model cont.
  10 cases differ by the gradually increasing max loads by 1 MPa
  Ex) case 1: nominal load 65 MPa & overload 125 MPa lasting 5 & 45 cycles
Retardation: the crack does not grow at all between 5000 and 15000 cycles
After 15000 cycles, the crack grows fast because underloads followed by overloads
The crack grows slowly after 20000 cycles because the number of cycles for overloads is reduced

## Slide 21: Health Monitoring Data and Loading Conditions
Noise and bias
  Deterministic bias: mm
  Uniformly distributed random noise: mm, mm
Data-driven approaches:
  Set 6 is prediction set for Paris model (all others are training set)
  Set 8 is prediction set for Huang’s model (all others are training set)
b=-0.003; v=0.001;
crackSimpleMeas=crackSimple + v*(2*rand(10,26)-1) + b;
crackHuangMeas=crackHuang + v*(2*rand(10,26)-1) + b;

## Slide 22: 3. Physics-based Prognostics

## Slide 23: Comparison of Physics-based Algorithms
Comparing physics-based prognostics algorithms for accuracy in parameter and RUL
focus on uncertainty and correlation in model parameters as well as model-form errors
Approaches
  likelihood: normal distribution, prior: uniform (see table in the next slide)
  Use 5000 samples to represent distributions (NLS, BM, PF)
NLS
  Identify mean and covariance  t-distribution to generate 5000 samples
BM
  6250 samples from MCMC and 1250 burn-in samples removed
PF
  5000 particles from prior distribution  resampled based on weights

## Slide 24: Prior Distributions

## Slide 25: Correlation in Prognostics
Performance of different algorithms can be evaluated based on their ability to identify model parameters
  Focus on physics-based prognostics is how to identify model parameters accurately with a smaller number of measured data
Correlation between parameters is the most challenging aspects
  Probabilistic identification of parameters (due to noise and model-form error)
  Marginal PDF is not accurate; Joint PDF (correlation) must be identified
  Without properly identifying the correlation, the predicted RUL can be significantly different from the real one
Even if the accurate value of each parameter may not be identified, the RUL prediction can be reliable
  all combinations of the correlated parameters can yield the same prediction

## Slide 26: Correlation between Model Parameters
Paris model parameters and are strongly correlated
  They can be identified with their correlation rather than individual values
  For a given , multiple can yield the same growth rate
  How can the change in correlation affect predictions
Paris model (logarithm)
Linear relationship b/w and

## Slide 27: Correlation between Model Parameters cont.
Correlation gradually changes as crack grows
  there is no deterministic relationship between parameters, and the relationship evolves as the crack size increases
  The slope changes w.r.t. the true value
  the true parameters can eventually be identified since the correlation converges to the true value by intersecting many correlation lines
True parameters can be obtained with only three exact degradation data
  Very small covariance

## Slide 28: Correlation between Model Parameters cont.
When data include noise, the linear relationship cannot be obtained
  Measurement at 2 different cycles  2 different slopes
No noise case:
  The intersection of two lines can identify the true model parameters
Noisy data case
  Due to uncertainty, line thickness is proportional to the level of noise
  Intersection is an area, not a point  uncertainty in the identified parameters
  Uncertainty increases when the level of noise is large and when the two slopes are not much different

## Slide 29: Correlation between Model Parameters cont.
Sensitivity of parameter identification (small noise case)
  : rounding error at 4th significant digit
  Even if the measured data have very small errors, the identified parameters are distributed in a very wide range.
  because only three data are used, and the slopes of correlation lines are very close to each other (the crack does not grow much during the three cycles)
  Too wide 90% PI, and median failed to follow the true degradation
  more data are required to identify the correlation well

## Slide 30: Correlation b/w Parameters and Loading
Black line: with correct loading
Red line: with smaller loading
A smaller loading leads to a larger parameter
That is, and are negatively correlated
prediction results from physics-based approaches can be accurate even under incorrect loadings because the model parameters are updated to the equivalent parameters to the incorrect loading

## Slide 31: Correlation b/w Parameters and Loading cont.
Use dataset 10 with a wrong load of
  Prognostics using NLS
  Overestimating , but degradation follows the true one

## Slide 32: Compensating for Model-Form Error
Correlation b/w load & parameter can be used for compensating model-form error
  the actual behavior of degradation is different from the physical model due to simplifications and assumptions in the physical model
  The error in model-form is often transferred to an error in loading conditions
Ex) Paris model with finite plate
  Correct stress intensity factor
  : apparent stress intensity factor, : correction factor
  The error in will be compensated by identifying equivalent parameters

## Slide 33: Correction Factor
The capability of compensating error in loading condition by identifying equivalent model parameters is limited to the case when the correction factor remains constant
  the correction factor is a function of crack size, and it will evolve as the crack grows

## Slide 34: Correlation b/w Initial Crack Size and Bias
Bias in data: sensor calibration error, unknown crack location, inclined crack orientation
Bias in measured data can be handled in physics-based approaches but not in data-driven approaches
  Constant bias won’t affect data-drive approaches
The bias can play an important role in physics-based method
  Positive bias: overestimating  underestimate
In order to identify bias, it is necessary to include it as a parameter

## Slide 35: Correlation b/w Initial Crack Size and Bias cont.
the bias is correlated with the initial crack size
Assume no noise in data
  For a given , infinitely possible combinations of and  linear correlation
Ex) and are known, , use 2 exact data to find and
  NLS identified and
Without bias correction
With bias correction

## Slide 36: Prior Information
Prior information: preexisting knowledge for unknown parameters
  expert’s opinion, previous experience or knowledge from similar systems
  Ex) Initial crack size: estimated from traditional NDT
  Ex) bias: measurement error from known crack size
  Ex) Model parameters and : from lab tests
Regression-based methods (LS, NLS)
  Frequentist’s method, only observed information is used, no prior information
Bayesian-based methods (BM, PF)
  Use prior (subjective) information, prior PDF
  Without prior, BM is equivalent to maximum likelihood estimate

## Slide 37: Prior information for Bayesian Inference
Performance of Bayesian inference
  depends on the uncertainty in prior and the variability in measured data
  Small uncertainty in the prior: measurement data may not contribute to improving the uncertainty in the posterior distribution (the prior distribution contributes the most to the posterior distribution)
  Small variability in measured data: not much use for the prior (the posterior distribution is dominated by measured data)
Effect of the prior distribution
  If the uncertainty in prior is small and it covers the true value of parameter, the prior can help accelerating the convergence of the posterior distribution
  If the uncertainty in prior distribution is too big, it will not help to reduce uncertainty in the posterior distribution
  non-informative prior: infinitely wide prior distribution, unnecessary to consider the prior distribution

## Slide 38: Prior information for Bayesian Inference cont.
Incorrect prior
  Wrong or inconsistent prior with measured data, it can prevent parameters from being accurately identified or slow down the estimation process
  Ex) but : the posterior will not include the true parameter no matter how many measured data are used
Use dataset 6 with up to 1500 cycles
  NLS show much larger uncertainty compared to BM and PF
NLS
BM
PF

## Slide 39: Prior information for Bayesian Inference cont.
Inferior performance of NLS can be explained by its inability to utilize the prior information
  Uniform prior cuts off the posterior distribution of BM and PF (make it narrower)

## Slide 40: Prior information for Bayesian Inference cont.
The influence of prior is gradually reduced as more data are used
  Increase # of date from 1500 to 2500 cycles
NLS
BM
PF

## Slide 41: Sampling Error
the prediction result from PF is worse than the other two
  accumulated sampling error during the updating process (particle depletion)
  only a few samples remain after 25 updating process for PF (blue dots)
particle depletion has been the major drawback of PF
  Possible remedy: add random samples from an arbitrary distribution during the prediction step so that duplicated particles are not generated
  can change probabilistic characteristics of parameters and can increase the variance of parameters
BM has sampling error due to the random walk process in MCMC sampling
  initial sample locations, the proposal distribution and the acceptance ratio have an effect on the sampling results
  marginal density function can be used for the proposal distribution

## Slide 42: Uncertainty Representation & Updating Process
NLS
  Deterministic parameters (mean) and added linear correlation based on the covariance matrix (use t-distribution)
  efficient for a strong linear correlation between unknown parameters
  not easy to find accurate relation for many unknown parameters
BM and PF
  a joint posterior distribution for unknown parameters (correlation can be well identified)
  Posterior distributions are not limited to standard distribution types (represented by samples)
  BM is faster when degradation model is given in a total form
  BM can be impractical when the degradation model is given in the rate form
  PF that is based on sequential updating process is only a practical method for the rate form of degradation model

## Slide 43: Results Summary
NLS can be a simple and accurate prediction method when the parameters are linearly correlated
  good with Gaussian noise in data and mildly nonlinear model
BM is an efficient method when the degradation model is given as a total form equation
  the degradation model has to be computationally inexpensive
  Grid approximation method for a small number of parameters
  Most practical problems use MCMC to generate samples
  Many MCMC samples are required for high-dimensional sampling
  Choosing appropriate options in MCMC is a real problem (initial parameter values and the width of proposal distribution)
  Too small width: not fully covering the target distribution
  Too large width: many duplications in samples by not accepting new samples
  the width of proposal distribution depends on the expected uncertainty in un-known parameters

## Slide 44: Results Summary cont.
PF is considered easy to use (not many options)
  state transition function as a physical model (rate form)
  particle depletion problem when many measured data are available

## Slide 45: 4. Data-driven Prognostics

## Slide 46: Comparison of Data-driven Algorithms
focuses are on the selection of model form, performance under noise and the number of training data
Gaussian process (GP) model
  Inputs: three degradation from previous time increments
  Global function: first-order polynomials, reflecting monotonicity of degradation
  Uncertainty: 5000 samples from Student’s t-distribution
Neural Network (NN) model
  Inputs: three degradation from previous time increments
  pure linear functions are used for both hidden and output layers (monotonicity)
  only one hidden node is considered
  Outlier: results beyond the bound of
  30 repetition for prediction intervals

## Slide 47: Simple Crack Growth Model
No training dataset, prediction dataset 6 up to 1500 cycles
uniformly distributed random noise
GP predicts slightly better than NN
  Higher (data/parameter) ratio for GP
v=0.001;
crackSimpleMeas=crackSimple(6,1:16) + v*(2*rand(1,16)-1);
GP with
NN with

## Slide 48: Simple Crack Growth Model cont.
prediction results using data up to 500 cycles with zero noise + training sets 5 and 7 (up to 2500 cycles)
  good prediction results in the interpolation regions
  GP works well in the interpolation region with small noise (accurate correlation)
  Beyond 2500 cycles, extrapolation and prediction deteriorates quickly
  NN works better for extrapolation, but accuracy is worse than GP
GP with
NN with

## Slide 49: Simple Crack Growth Model cont.
Large noise
  prediction performance of GP is significantly deteriorated (correlation cannot clearly be identified)
  GP performance is improved with
  the optimum value of the hyper-parameter remains the same as the initial value
  the prediction results totally depend on the linear global function
GP with
GP with

## Slide 50: Simple Crack Growth Model cont.
NN outperformed GP
  When there is a large level of noise in data, having training sets may not help much in improving prediction accuracy
  when the level of noise is large, it may help to use time/cycle as an input in NN in-stead of using the previous data as input
NN with
time as input and sigmoid function

## Slide 51: Results Summary
GP is an efficient and accurate prediction method when a small number of data are given with a small level of noise
  It is, however, not an easy task to build a proper correlation matrix since not only a large level of noise but also a large number of data adversely affect handling the correlation matrix
NN is less sensitive in the level of noise
  a large number of data increase the accuracy in prediction results

## Slide 52: 5. Comparison between Physics-based and Data-driven Prognostics

## Slide 53: Comparison Using Huang’s Model
PF with distributed initial damage size
PF with true value of initial damage size
NN with ns=8 training Sets 2, 7 and 9
NN with ns=23 training Sets 2, 7 and 9 and loading conditions

## Slide 54: Comparison Using Huang’s Model cont.
Rate form: NLS and BM are not effective
PF for physics-based model and NN for data-driven model
PF using data up to 16,000 cycles (7 parameters, 5000 particles)
  Using accurate initial damage is important for the accuracy
NN using 3 training data sets
  Proximity between training data (7, 9) and prediction data set (8)
  22 out of 30 repetitions failed to satisfy 2 regulations
  Loading information can improve the accuracy
With more training data sets and loading information, data-driven approaches can outperform physics-bade approaches

## Slide 55: Summary
Physics-based methods
  less affected by the level of noise and model complexity
  employed only when a physical model and loading conditions are available
  NLS works favorable for a linear correlation case
  PF has a wide range of applications
  BM is fast when the expression of posterior distribution is available explicitly
Data-driven methods
  GP works well when the covariance function is well-defined, such as the case of low noise in data and simple behavior of the damage growth
  GP can outperform other algorithms if interpolation conditions can be considered with the given information
  GP is easy to implement and quick to calculate, which gives prediction results with interval within around 2 seconds

## Slide 56: Summary cont.
Data-driven methods
  NN does not require choosing various tuning parameters
  the computational cost depends on each training case
  NN is advantageous for cases with high levels of noise and complex models with many training data sets
When loading conditions and physical models are not available
  prediction can be done by using data-driven approaches with at least three data sets, and loading conditions improve the prediction results
Hybrid approaches or fusion methods that combine the two approaches or prediction results can be considered to improve the prediction performance